Korapox 439

Spectrum Report

Counts per second

Energy KeV

Full scale: 5400 cps

Counts per second

Full scale: 5400 cps

|  | Element | Counts per second |
| --- | --- | --- |
| C | Carbon | 4882 |
| O | Oxygen | 1584 |
| Si | Silica | 613 |
| Cl | Chlorine | 1106 |

Energy KeV